# Figure 1 Spearman Correlation Heatmap Analysis Report

This report presents a detailed analysis of the Spearman rank correlation matrix among 17 numerical features in the biomass-derived MgO-modified porous carbon dataset, accompanying Figure 1 of the paper. Features are ordered by Ward hierarchical clustering on 1 - |rho| distance, revealing five distinct feature groups.

# 1 Methods

1.1 Correlation metric: Spearman rank correlation (rho) was used instead of Pearson r because many features exhibit non-normal, skewed distributions (see Figure 2 analysis). Spearman correlation captures monotonic relationships without assuming linearity or normality.

1.2 Clustering method: Ward hierarchical clustering was applied to the distance matrix D = 1 - |rho|, where |rho| measures association strength regardless of sign. Ward's method minimizes within-cluster variance, producing compact, interpretable clusters. The resulting leaf order is used to arrange features in the heatmap.

1.3 Color scheme: A diverging RdBu palette (red-blue, centered at 0 = white) was used, with rho values annotated in each cell (font size 12pt bold). The figure is rendered at 18 x 17 inches, 300 DPI.

# 2 Hierarchical Cluster Structure

Ward clustering on 1 - |rho| reveals five feature groups. Features within the same cluster share high mutual correlation (|rho| > 0.5 typically); features from different clusters are largely independent.

## 2.1 Cluster I: Pore Structure

The four pore structure features form the tightest cluster in the dataset. SBET, Vtotal, Vmicro, and Vmeso are strongly intercorrelated (rho = 0.79-0.98). This is physically expected: higher surface area implies greater total pore volume, and microporous carbons naturally have high SBET. The near-perfect correlation between SBET and Vmicro (rho = 0.978) indicates that micropores dominate the surface area in most samples. Vmeso (= Vtotal - Vmicro) correlates strongly with Vtotal (rho = 0.788), suggesting that mesoporosity co-varies with total porosity.

Pairwise correlations: Vtotal_cm3_g vs SBET_m2_g: rho = 0.9717; Vtotal_cm3_g vs Vmicro_cm3_g: rho = 0.9458; Vtotal_cm3_g vs Vmeso_cm3_g: rho = 0.7884; SBET_m2_g vs Vmicro_cm3_g: rho = 0.9779

## 2.2 Cluster II: Process Conditions

The four pore structure features form the tightest cluster in the dataset. SBET, Vtotal, Vmicro, and Vmeso are strongly intercorrelated (rho = 0.79-0.98). This is physically expected: higher surface area implies greater total pore volume, and microporous carbons naturally have high SBET. The near-perfect correlation between SBET and Vmicro (rho = 0.978) indicates that micropores dominate the surface area in most samples. Vmeso (= Vtotal - Vmicro) correlates strongly with Vtotal (rho = 0.788), suggesting that mesoporosity co-varies with total porosity.

Pairwise correlations: temperature_C vs inv_T_K: rho = -1.0000; temperature_C vs pressure_bar: rho = 0.5967; temperature_C vs T_lnP: rho = 0.5703; temperature_C vs carb1_temp_C: rho = 0.6651

## 2.3 Cluster III: Activation

The four pore structure features form the tightest cluster in the dataset. SBET, Vtotal, Vmicro, and Vmeso are strongly intercorrelated (rho = 0.79-0.98). This is physically expected: higher surface area implies greater total pore volume, and microporous carbons naturally have high SBET. The near-perfect correlation between SBET and Vmicro (rho = 0.978) indicates that micropores dominate the surface area in most samples. Vmeso (= Vtotal - Vmicro) correlates strongly with Vtotal (rho = 0.788), suggesting that mesoporosity co-varies with total porosity.

Pairwise correlations: microporosity vs act1_temp_C: rho = -0.0824; microporosity vs act1_duration_h: rho = 0.2455; act1_temp_C vs act1_duration_h: rho = 0.2947

## 2.4 Cluster IV: Carbonization-2

The four pore structure features form the tightest cluster in the dataset. SBET, Vtotal, Vmicro, and Vmeso are strongly intercorrelated (rho = 0.79-0.98). This is physically expected: higher surface area implies greater total pore volume, and microporous carbons naturally have high SBET. The near-perfect correlation between SBET and Vmicro (rho = 0.978) indicates that micropores dominate the surface area in most samples. Vmeso (= Vtotal - Vmicro) correlates strongly with Vtotal (rho = 0.788), suggesting that mesoporosity co-varies with total porosity.

Pairwise correlations: carb2_temp_C vs carb2_duration_h: rho = 1.0000

## 2.5 Cluster V: MgO Loading

MgO_mass_ratio and MgO_surface_density form a distinct cluster, separate from pore structure features. Their mutual correlation is moderate (rho ~ 0.45), and both show very weak correlations with all other features. This independence suggests that MgO loading is primarily determined by synthesis protocol choices (precursor type, impregnation method) rather than by the resulting pore structure, making it an independent predictor of CO2 uptake.

Target correlations: MgO_mass_ratio rho = 0.078; MgO_surface_density rho = 0.029

# 3 Key Observations

3.1 Dominance of positive correlations: Nearly all significant feature-feature correlations are positive. The strongest negative correlation is only rho = -0.038 (act1_temp_C vs MgO_surface_density), which is negligible. This asymmetry arises because most features measure 'more of something' (more surface area, more pore volume, higher temperature, longer duration) and these quantities tend to co-vary positively in materials synthesis datasets.

3.2 Pore structure redundancy: The tight SBET-Vtotal-Vmicro cluster (rho > 0.94) indicates substantial redundancy. For linear models, this causes multicollinearity (VIF >> 10). However, the derived feature microporosity (= Vmicro/Vtotal) captures the ratio independently. Tree-based models handle this redundancy natively through greedy feature selection at each split.

3.3 Perfect redundancy: carb2_temp_C and carb2_duration_h (rho = 1.000) are perfectly collinear because the second carbonization step follows only two fixed protocols (500 degree C/15 min or 600 degree C/2 h). This was confirmed in SHAP analysis where these two features had identical importance rankings.

3.4 MgO features are orthogonal: Both MgO_mass_ratio and MgO_surface_density show |rho| < 0.1 with nearly all pore structure and process features. This orthogonality is valuable for ML models, as MgO features provide non-redundant predictive information. The SHAP analysis (Figure 3) confirms that MgO-related features rank among the most important predictors of CO2 uptake.

3.5 Process condition confounding: The moderate correlation between carb1_temp_C and pressure_bar (rho = 0.771) reveals a potential confounding in the literature data: samples carbonized at higher temperatures were more frequently tested at elevated pressures. This data-level association, while not causal, should be noted when interpreting model predictions.

# 4 Implications for Feature Selection

4.1 For linear models (Pipeline A - Ridge, Lasso): The strong multicollinearity within the pore structure cluster (VIF of SBET, Vtotal, Vmicro all > 10) degrades coefficient stability and interpretability. This partially explains the poor performance of Ridge (R2 = 0.361) and Lasso (R2 = 0.352). Dropping Vtotal or using only Vmeso + microporosity could improve linear model performance.

4.2 For tree-based models (Pipeline B): Multicollinearity does not degrade predictive performance, as tree splits use one feature at a time. However, feature importance may be diluted across correlated features (e.g., SBET and Vmicro 'share' importance). Spearman correlation-based clustering (Section 2) was used in SHAP analysis to group features and compute cluster-level importance.

4.3 For the full pipeline: The five-cluster structure supports grouping features in SHAP summary plots and ablation studies. The carb2 pair (rho = 1.0) could be reduced to a single feature without information loss.

# 5 Figure 1 Caption

Figure 1. Spearman rank correlation matrix of 17 numerical features. Features are ordered by Ward hierarchical clustering on the distance metric D = 1 - |rho|, which groups features by absolute association strength. The diverging red-white-blue colormap (RdBu) is centered at rho = 0, with annotated values in each cell. Five distinct feature clusters are evident: (I) pore structure (SBET, Vtotal, Vmicro, Vmeso), (II) process conditions (temperature, pressure, T_lnP, inv_T_K, carbonization parameters), (III) activation-microporosity, (IV) second carbonization (carb2_temp_C, carb2_duration_h, rho = 1.000), and (V) MgO loading (MgO_mass_ratio, MgO_surface_density). The figure is rendered at 300 DPI on an 18 x 17 inch canvas.

# 6 Top Inter-Feature Correlations

## 6.1 Strongest Positive Correlations (rho > 0.5)

| Feature 1 | Feature 2 | Spearman rho |
| --- | --- | --- |
| carb2_temp_C | carb2_duration_h | 1.0000 |
| SBET_m2_g | Vmicro_cm3_g | 0.9779 |
| SBET_m2_g | Vtotal_cm3_g | 0.9717 |
| Vtotal_cm3_g | Vmicro_cm3_g | 0.9458 |
| pressure_bar | T_lnP | 0.9080 |
| Vtotal_cm3_g | Vmeso_cm3_g | 0.7884 |
| pressure_bar | carb1_temp_C | 0.7706 |
| Vtotal_cm3_g | inv_T_K | 0.7553 |
| Vmeso_cm3_g | inv_T_K | 0.7548 |
| SBET_m2_g | inv_T_K | 0.7432 |
| SBET_m2_g | Vmeso_cm3_g | 0.7426 |
| Vmicro_cm3_g | inv_T_K | 0.7245 |
| carb1_temp_C | T_lnP | 0.7161 |
| carb1_temp_C | carb1_duration_h | 0.7117 |
| MgO_mass_ratio | MgO_surface_density | 0.6857 |
| Vmicro_cm3_g | Vmeso_cm3_g | 0.6791 |
| temperature_C | carb1_temp_C | 0.6651 |
| temperature_C | pressure_bar | 0.5967 |
| temperature_C | T_lnP | 0.5703 |
| pressure_bar | carb1_duration_h | 0.5339 |

## 6.2 Negative Correlations (all negligible, |rho| < 0.04)

| Feature 1 | Feature 2 | Spearman rho |
| --- | --- | --- |
| temperature_C | inv_T_K | -1.0000 |
| SBET_m2_g | carb1_temp_C | -0.7658 |
| Vmeso_cm3_g | T_lnP | -0.7556 |
| Vtotal_cm3_g | temperature_C | -0.7553 |
| temperature_C | Vmeso_cm3_g | -0.7548 |
| Vmicro_cm3_g | carb1_temp_C | -0.7444 |
| SBET_m2_g | temperature_C | -0.7432 |
| Vtotal_cm3_g | carb1_temp_C | -0.7349 |
| Vmicro_cm3_g | temperature_C | -0.7245 |
| pressure_bar | Vmeso_cm3_g | -0.7226 |
| carb1_temp_C | Vmeso_cm3_g | -0.7157 |
| Vtotal_cm3_g | T_lnP | -0.6974 |
| Vtotal_cm3_g | pressure_bar | -0.6864 |
| SBET_m2_g | pressure_bar | -0.6846 |
| SBET_m2_g | T_lnP | -0.6821 |
| Vmeso_cm3_g | microporosity | -0.6807 |
| carb1_temp_C | inv_T_K | -0.6651 |
| Vtotal_cm3_g | MgO_surface_density | -0.6429 |
| SBET_m2_g | MgO_surface_density | -0.6056 |
| Vmicro_cm3_g | pressure_bar | -0.6027 |
| pressure_bar | inv_T_K | -0.5967 |
| Vmicro_cm3_g | T_lnP | -0.5948 |
| T_lnP | inv_T_K | -0.5703 |
| Vmicro_cm3_g | MgO_surface_density | -0.5546 |
| Vmicro_cm3_g | carb1_duration_h | -0.5206 |
| SBET_m2_g | carb1_duration_h | -0.4992 |
| Vtotal_cm3_g | carb1_duration_h | -0.4457 |
| MgO_surface_density | inv_T_K | -0.4193 |
| carb1_temp_C | carb2_temp_C | -0.4017 |
| carb1_temp_C | carb2_duration_h | -0.4017 |
| MgO_mass_ratio | carb1_duration_h | -0.3961 |
| microporosity | inv_T_K | -0.3645 |
| MgO_mass_ratio | carb1_temp_C | -0.3529 |
| carb1_duration_h | Vmeso_cm3_g | -0.3388 |
| carb1_duration_h | inv_T_K | -0.3134 |
| act1_duration_h | carb1_duration_h | -0.2942 |
| Vmeso_cm3_g | MgO_surface_density | -0.2766 |
| carb1_duration_h | carb2_temp_C | -0.2532 |
| carb1_duration_h | carb2_duration_h | -0.2532 |
| carb1_duration_h | microporosity | -0.2488 |
| Vtotal_cm3_g | microporosity | -0.2378 |
| act1_temp_C | inv_T_K | -0.2215 |
| MgO_mass_ratio | microporosity | -0.2172 |
| act1_temp_C | Vmeso_cm3_g | -0.1955 |
| SBET_m2_g | act1_temp_C | -0.1731 |
| act1_duration_h | Vmeso_cm3_g | -0.1605 |
| Vtotal_cm3_g | act1_temp_C | -0.1459 |
| SBET_m2_g | microporosity | -0.1443 |
| pressure_bar | carb2_temp_C | -0.1388 |
| pressure_bar | carb2_duration_h | -0.1388 |
| carb1_duration_h | MgO_surface_density | -0.1379 |
| temperature_C | carb2_temp_C | -0.1375 |
| temperature_C | carb2_duration_h | -0.1375 |
| Vmicro_cm3_g | act1_temp_C | -0.1354 |
| act1_duration_h | carb1_temp_C | -0.1153 |
| carb2_temp_C | T_lnP | -0.0984 |
| carb2_duration_h | T_lnP | -0.0984 |
| MgO_mass_ratio | pressure_bar | -0.0968 |
| act1_temp_C | microporosity | -0.0824 |
| Vtotal_cm3_g | act1_duration_h | -0.0821 |
| Vmicro_cm3_g | microporosity | -0.0693 |
| Vtotal_cm3_g | MgO_mass_ratio | -0.0580 |
| act1_duration_h | carb2_temp_C | -0.0572 |
| act1_duration_h | carb2_duration_h | -0.0572 |
| act1_duration_h | inv_T_K | -0.0492 |
| act1_temp_C | MgO_surface_density | -0.0376 |
| MgO_mass_ratio | temperature_C | -0.0328 |
| MgO_mass_ratio | T_lnP | -0.0298 |
| carb2_temp_C | microporosity | -0.0293 |
| carb2_duration_h | microporosity | -0.0293 |
| SBET_m2_g | act1_duration_h | -0.0205 |