# Figure 2 Box Plot Analysis Report

This report analyzes the distribution characteristics of 17 numerical features in the biomass-derived MgO-modified porous carbon dataset, serving as supporting documentation for Figure 2 of the paper. All features are Z-score standardized and grouped into 5 domains by domain knowledge, distinguished by color.

# 1 Data Overview

Dataset: 341 samples, 19 original numerical features. After excluding 2 zero-variance features (act2_temp_C, act2_duration_h), 17 features are included in the box plot analysis.

Target variable: CO2 uptake (T = 0 degree C, P = 1 bar), range 1.3-292.7 mg/g, mean 99.6 +/- 62.4 mg/g.

# 2 Group-wise Distribution Analysis

## 2.1 Pore Structure

Characterize the specific surface area and pore volume of porous carbon. SBET ranges broadly (9.8-1623 m2/g, CV=0.63), reflecting the diversity of precursors and activation conditions. Vmeso (mesopore volume) shows right-skewed distribution (skew=1.71). Most samples are microporous (microporosity median 0.69), while a few samples have near-zero microporosity, indicating wide pore structure tunability.

| Feature | Mean | Std | CV | Skewness | Missing % | Outliers (¦Z¦>3) |
| --- | --- | --- | --- | --- | --- | --- |
| SBET_m2_g | 728.73 | 462.01 | 0.634 | 0.512 | 0.0% | 0 (0.0%) |
| Vtotal_cm3_g | 0.44 | 0.23 | 0.535 | 0.300 | 0.0% | 1 (0.3%) |
| Vmicro_cm3_g | 0.29 | 0.17 | 0.573 | 0.691 | 0.0% | 0 (0.0%) |
| Vmeso_cm3_g | 0.15 | 0.11 | 0.724 | 1.707 | 0.0% | 3 (0.9%) |
| microporosity | 0.69 | 0.19 | 0.270 | -0.120 | 0.0% | 2 (0.6%) |

## 2.2 MgO Loading

MgO_mass_ratio has a median of only 0.25, with strong right skew (skew=0.71), indicating low MgO loading in most samples. MgO_surface_density (MgO mass per unit surface area) has a CV of 2.30 and skew of 7.49, with extreme outliers (max 33.9 g/m2), reflecting highly variable MgO dispersion uniformity on the carbon skeleton.

| Feature | Mean | Std | CV | Skewness | Missing % | Outliers (¦Z¦>3) |
| --- | --- | --- | --- | --- | --- | --- |
| MgO_mass_ratio | 0.44 | 0.33 | 0.757 | 0.707 | 0.0% | 0 (0.0%) |
| MgO_surface_density | 1.32 | 3.02 | 2.295 | 7.489 | 0.0% | 6 (1.8%) |

## 2.3 Process Conditions

temperature_C (adsorption temperature) is dominated by 25 degree C (median=25), with a few samples tested at elevated temperatures (max 289 degree C), resulting in strong right skew (2.28). pressure_bar mainly clusters around 1 bar, with a right tail from high-pressure conditions (max 15 bar). T_lnP and inv_T_K are derived composite features with concentrated distributions.

| Feature | Mean | Std | CV | Skewness | Missing % | Outliers (¦Z¦>3) |
| --- | --- | --- | --- | --- | --- | --- |
| temperature_C | 46.11 | 58.31 | 1.265 | 2.278 | 0.0% | 10 (2.9%) |
| pressure_bar | 1.19 | 1.46 | 1.224 | 4.189 | 0.0% | 3 (0.9%) |
| T_lnP | 1.54 | 34.06 | 22.178 | 0.457 | 0.0% | 8 (2.3%) |
| inv_T_K | 0.00 | 0.00 | 0.137 | -1.479 | 0.0% | 6 (1.8%) |

## 2.4 Activation Parameters

act1_temp_C and act1_duration_h are available only for samples undergoing the first activation step (248/341, 27.3% missing). Temperature concentrates at 700-850 degree C, duration at 2 h, with narrow distributions (CV=0.08-0.16). act2 parameters were excluded due to zero variance (only 9 samples with second activation).

| Feature | Mean | Std | CV | Skewness | Missing % | Outliers (¦Z¦>3) |
| --- | --- | --- | --- | --- | --- | --- |
| act1_temp_C | 718.83 | 117.50 | 0.163 | -2.314 | 27.3% | 9 (2.6%) |
| act1_duration_h | 1.96 | 0.15 | 0.078 | -3.146 | 27.3% | 11 (3.2%) |

## 2.5 Carbonization Parameters

carb1_temp_C shows a bimodal distribution: low temperature (~160 degree C, hydrothermal) and high temperature (600-900 degree C, conventional pyrolysis), with only 1.5% missing. carb2 parameters have 49% missing, indicating ~half of samples lacked a second carbonization step. carb2_temp_C concentrates at 500-600 degree C (CV=0.05). Carbonization duration is typically 1-2 h, with a few carb1_duration_h outliers (max 4 h).

| Feature | Mean | Std | CV | Skewness | Missing % | Outliers (¦Z¦>3) |
| --- | --- | --- | --- | --- | --- | --- |
| carb1_temp_C | 433.54 | 269.10 | 0.621 | 0.119 | 1.5% | 0 (0.0%) |
| carb1_duration_h | 1.34 | 0.58 | 0.431 | 2.725 | 15.2% | 6 (1.8%) |
| carb2_temp_C | 590.23 | 29.78 | 0.050 | -2.734 | 49.0% | 17 (5.0%) |
| carb2_duration_h | 1.83 | 0.52 | 0.285 | -2.734 | 49.0% | 17 (5.0%) |

# 3 Overall Distribution Characteristics

3.1 Non-normality: Most features exhibit non-normal distributions. MgO_surface_density (skew=7.49), pressure_bar (4.19), carb1_duration_h (2.73), and temperature_C (2.28) show strong right skew, reflecting the presence of samples with extreme synthesis/testing conditions. Carbonization/activation temperature parameters concentrate at a few discrete values due to limited process types, resulting in discrete rather than continuous distributions.

3.2 Missing data patterns: Missing values arise from optional process steps. When a sample did not undergo a specific activation/carbonization step, the corresponding temperature and duration features are recorded as NaN (rather than 0), preserving the semantic meaning of step not performed. Box plots are drawn using only non-missing values.

3.3 Outliers: MgO_surface_density has the most outliers (|Z|>3: 1.8%), corresponding to samples with extremely high MgO loading but low specific surface area. temperature_C has 2.9% outliers from non-ambient adsorption test conditions. These outliers represent genuine extreme synthesis/testing conditions and should not be removed.

# 4 Implications for ML Modeling

4.1 Necessity of nonlinear models: The non-normal, skewed feature distributions further support the finding that tree-based ensemble models (RF, XGBoost, LightGBM, GBDT) and TabPFN substantially outperform linear models (Ridge, Lasso), with a nonlinear-linear R2 gap of 0.592.

4.2 Missing value handling: Pipeline B (tree models) natively supports missing values; Pipelines A and C use SimpleImputer. The missingness in process parameters is structural (not random), with the step-performed-or-not information already captured by categorical variables (act1_type, etc.).

4.3 Feature skewness and transformations: The extreme skewness of MgO_surface_density (7.49) suggests that log1p transformation in Pipeline C (SVR/GPR) may improve performance; tree-based models are insensitive to this.

4.4 Zero-variance features: act2 temperature/duration were excluded because only 9 samples had values, creating information redundancy with their categorical counterpart act2_type (none vs. H3PO4).

# 5 Figure 2 Caption

Figure 2. Standardized box plots of 17 numerical features. Each box represents the interquartile range (IQR, Q1-Q3); the line inside the box marks the median (Q2); whiskers extend to the farthest point within Q1-1.5*IQR and Q3+1.5*IQR; points beyond whiskers are outliers. The x-axis is Z-score (subtract mean, divide by standard deviation) to enable cross-feature comparison. Colors denote five feature groups: blue - pore structure, orange - MgO loading, green - process conditions, purple - activation parameters, gold - carbonization parameters.